FEATURES

1. High ripple current and Long life, 105℃ 12000Hrs耐高纹波  105℃ 12000小时产品

2.For Electronic Ballast,power supply专为节能灯设计制造

SPECIFICATIONS

| Item 项目 | Performance characteristics 主要特性 |
| --- | --- |
| Rated Working Voltage Range 额定工作电压范围 | 160 to 450V DC |
| Operation Temperature Range 使用温度范围 | -25 to ～105℃ |
| Nominal Capacitance Range 标称容量 | 1.0 to 220μF |
| Capacitance Tolerance 电容量允许偏差 | ±20%(120Hz,+20℃) |
| Leakage Current 漏电流 | 1≤0.02CV+5(μA) after 2 minutes application of rated voltage 额定电压2分钟测试值 |
| Dissipation Factor tanδ (120Hz,+20℃) 损耗正切值tanδ | Working voltage(V) | 160 | 200 | 250 | 350 | 400 | 450 |
|  | tanδ(max) | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.10 |
| Surge Voltage 浪涌电压 | Working voltage(V) | 160 | 200 | 250 | 350 | 400 | 450 |
|  | Surge voltage(V) | 200 | 250 | 300 | 400 | 450 | 500 |
| Multiplier for Ripple Current 修正糸数 | Frequency Coefficient |  |  |  |  |  |  |
|  | Frequency (Hz) | 120 | 1K | 10K | 100K |  |  |  |  |  |  |
|  | Coefficient | 0.50 | 0.80 | 0.90 | 1.00 |  |  |  |  |  |  |
| Low Temperature Characteristics 低温特性 | Impedance ratio max. at 120Hz |  |  |  |  |  |  |
|  | Working voltage(V) | 160 | 200 | 250 | 350 | 400 | 450 |
|  | Z-25℃/ Z+20℃ | 3 | 3 | 3 | 5 | 5 | 5 |
| High Temperature Loading 高温负荷 | Test conditions 试验条件 Duration : 12000 hours Ambient temperature : +105℃ Applied voltage : DC bias voltage puls the rated ripple current Post test requirements at +20℃ 试验完毕在20℃测试应满足 Leakage current :≤Initial specified value Capacitance change :≤±20% of initial measured value tan δ :≤200% of initial specified value |
| Shelf Life 贮存寿命 | Test conditions 试验条件 Duration : 1000 hours Ambient temperature : +105℃ Applied voltage : (None) Post test requirements at +20℃ 试验完毕在20℃测试应满足 Leakage current :≤Initial specified value Capacitance change :≤±20% of initial measured value tan δ :≤200% of initial specified value |
| Others 其它 | JIS C-5141 JIS C-5102 |

## CASE SIZE TABLE

DIMESIONS                                                                   φD×L(mm)

| Voltage Cap.(μF) Code | 160V | 200V | 250V |
| --- | --- | --- | --- |
|  | Case Size (mm) | Allowableripple (mA) | Case Size (mm) | Allowable ripple (mA) | Case Size (mm) | Allowable ripple (mA) |
| 1.0 | 105 |  | 20/40 |  | 21/42 |  | 22/44 |
| 1.5 | 155 |  | 25/50 |  | 27/54 |  | 27/54 |
| 2.2 | 225 |  | 30/60 |  | 34/68 |  | 35/70 |
| 3.3 | 335 |  | 36/72 |  | 28/75 | 8×16 | 38/75 |
| 4.7 | 475 |  | 40/80 | 8×16 | 28/95 | 8×16 | 28/95 |
| 6.8 | 685 | 8×16 | 45/90 | 10×16 | 51/102 | 8×16 | 51/102 |
|  |  |  |  |  |  | 10×16 |  |
| 10 | 106 | 10×16 | 125/250 | 8×16 | 125/250 | 10×16 | 140/280 |
|  |  |  |  | 10×16 |  | 10×20 |  |
| 15 | 156 | 8×16 | 190/380 | 10×16 | 190/380 | 10×20 | 210/420 |
|  |  | 10×16 |  | 10×20 |  | 13×16 |  |
| 22 | 226 | 10×16 | 250/500 | 10×20 | 250/500 | 13×16 | 250/500 |
|  |  | 10×20 |  | 13×16 |  | 13×21 |  |
| 33 | 336 | 10×20 | 250/500 | 13×16 | 300/600 | 13×21 | 300/600 |
|  |  | 13×16 |  | 13×21 |  | 13×25 |  |
| 47 | 476 | 13×21 | 330/660 | 13×21 | 330/660 | 13×25 | 360/720 |
|  |  | 13×25 |  | 13×25 |  | 16×26 |  |
| 68 | 686 | 13×25 | 380/760 | 13×25 | 380/760 | 16×26 | 460/920 |
|  |  | 16×26 |  | 16×22 |  | 18×22 |  |
| 100 | 107 | 16×26 | 560/1120 | 16×26 | 560/1120 | 16×31 | 600/1200 |
|  |  | 18×22 |  | 18×22 |  | 18×26 |  |
| 150 | 157 | 16×31 | 680/1350 | 16×31 | 680/1360 | 16×36 | 750/1500 |
|  |  | 18×26 |  | 18×26 |  | 18×31 |  |
| 220 | 227 | 16×31 | 700/1400 | 16×36 | 850/1700 | 20×41 | 900/1800 |
|  |  | 18×26 |  | 18×31 |  | 22×36 |  |

Allowable Ripple Current (mA rms) at 105℃,120Hz / Allowable Ripple urrent (mA rms) at 105℃ 100kHz

φD×L(mm)

| Voltage Cap.(μF) Code | 350V | 400V | 450V |
| --- | --- | --- | --- |
|  | 2V | 2G | 2W |
| 1.0 | 105 |  | 26/53 |  | 28/56 |  | 30/60 |
| 1.2 | 125 |  | 28/56 |  | 29/58 |  | 34/68 |
| 1.5 | 155 |  | 29/58 |  | 30/60 |  | 36/72 |
| 1.8 | 185 |  | 30/60 |  | 35/70 | 8×16 | 28/76 |
| 2.2 | 225 | 8×16 | 32/65 | 8×16 | 28/75 | 10×16 | 40/80 |
| 3.3 | 335 | 10×16 | 40/80 | 10×16 | 45/90 | 10×16 | 48/95 |
|  |  |  |  |  |  | 10×20 |  |
| 4.7 | 475 | 10×16 | 50/100 | 10×16 | 75/150 | 10×20 | 55/110 |
|  |  |  |  | 10×20 |  | 10×20 |  |
| 6.8 | 685 | 10×16 | 110/220 | 10×20 | 110/220 | 13×16 | 75/150 |
|  |  |  |  | 13×16 |  | 13×21 |  |
| 10 | 106 | 10×16 | 140/280 | 13×16 | 140/280 | 13×21 | 160/320 |
|  |  | 10×20 |  | 13×21 |  | 13×25 |  |
| 15 | 156 | 10×20 | 160/320 | 13×21 | 190/380 | 13×25 | 240/480 |
|  |  | 13×16 |  | 13×25 |  | 16×26 |  |
| 22 | 226 | 13×16 | 175/350 | 13×25 | 215/430 | 16×26 | 280/560 |
|  |  | 13×25 |  | 16×22 |  | 16×31 |  |
| 33 | 336 | 13×25 | 250/500 | 16×26 | 320/640 | 16×31 | 350/700 |
|  |  | 16×26 |  | 16×31 |  | 18×31 |  |
| 47 | 476 | 16×26 | 330/660 | 18×31 | 420/840 | 18×31 | 440/880 |
|  |  | 16×31 |  | 18×26 |  | 18×36 |  |
| 68 | 686 | 16×31 | 425/850 | 18×31 | 500/1000 | 20×41 | 550/1100 |
|  |  | 18×31 |  | 18×36 |  | 22×36 |  |

Allowable Ripple Current (mA rms) at 105℃,120Hz / Allowable Ripple urrent (mA rms) at 105℃ 100kHz