FEATURES

1. Low impedance for high frequency. 高频低阻抗

2. Life time: 2000 hours at 105℃. 寿命：105℃达2000小时.

SPECIFICATIONS  规格表

| Item项目 | Performance characteristics 主要特性 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Rated Working Voltage Range 额定工作电压范围. | 6.3 to100V |  |  |  |  |  |  |  |  |  | 160 to450V |  |  |  |  |  |  |  |  |  |  |  |  |  |
| OperationTemperature Range 使用温度范围 | -40 to +105℃ |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Nominal Capacitance Range 标称容量 | 0.47 to 4700μF |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Capacitance Tolerance 电容量允许偏差 | ±20%(120Hz,+20℃) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Leakage Current 漏电流 | V≤100V,I≤0.01CV or 3(μA) after 2 minutes whichever is greater measured with rated working voltage applied at +20℃ 20℃,升到额定电压后两分钟读数，取较大者。 |  |  |  |  |  |  |  |  |  |  |  | V≥160V,I≤0.02CV or 10(μA) after 2 minutes whichever is greater measured with rated working voltage applied at +20℃ 20℃,升到额定电压后两分钟读数，取较大者。 |  |  |  |  |  |  |  |  |  |  |  |
| Dissipation Factor tanδ (120Hz,+20℃) 损失角正切值. | Working voltage(V) | 6.3 |  | 10 |  | 16 |  | 25 |  | 35 |  |  |  | 50 |  | 63 |  | 100 |  | 160-250 |  |  | 400-450 |  |
|  | tanδ(max.) | 0.22 |  | 0.19 |  | 0.16 |  | 0.14 |  | 0.12 |  |  |  | 0.10 |  | 0.09 |  | 0.08 |  | 0.20 |  |  | 0.24 |  |
| Low Temperature Characteristics 低温特性 | Impedance ratio max. at 120Hz，120Hz时，最大阻抗比率. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Working voltage(V) |  | 6.3 |  | 10 |  | 16 |  | 25 |  |  | 35 |  |  | 50 |  | 63 |  | 100 |  | 160-250 | 450 |  | 450 |
|  | Z-40℃/ Z+20℃ |  | 8 |  | 6 |  | 4 |  | 3 |  |  | 3 |  |  | 3 |  | 3 |  | 3 |  | 4 | 6 |  | 6 |
| High Temperature Loading 高温负荷 | Test conditions 试验条件 Duration : 2000 hours Ambient temperature : +105℃ Applied voltage : Rated DC working voltage. Post test requirements at +20℃ 试验完毕在20℃测试应满足条件 Leakage current : ≤Initial specified value Capacitance change : ≤±20% of initial measured value tan δ : ≤150% of initial specified value |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Shelf Life 高温贮存 | Test conditions Post test requirements at +20℃ 试验条件 Duration : 1000 hours Ambient temperature : +105℃ Applied voltage : (None) 试验完毕在20℃测试应满足条件. Leakage current : ≤200%Initial specified value Capacitance change : ≤±20% of initial measured value tan δ : ≤150% of initial specified value |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Others 其它 | JIS C-5141 JIS C-5102 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

CASE SIZE TABLE  外型尺寸图

Temperature Multipliers 温度系数

| Temperature(℃) | -75 | +85 | +105 |
| --- | --- | --- | --- |
| Coefficient | 1.9 | 1.6 | 1.0 |

# RIPPLE CURRENT COEFEIENT

Frequency Multipliers

纹波电流频率调整系数

| Temperature(℃) | 120Hz | 1k Hz | 10k Hz | 100k Hz |
| --- | --- | --- | --- | --- |
| Coefficient | 0.4 | 0.7 | 0.85 | 1.0 |

# STANDARD RATINGS

| Voltage Item Cap.( μF) | 6.3V |  |  | 10V |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 100 |  |  |  | 5×11 | 161 | 0.600 |
| 120 |  |  |  | 5×11 | 161 | 0.600 |
| 150 | 5×11 | 161 | 0.420 | 6.3×11 | 250 | 0.320 |
| 220 | 6.3×11 | 246 | 0.320 | 6.3×11 | 255 | 0.220 |
| 330 | 6.3×11 | 246 | 0.320 | 8×12 | 391 | 0.140 |
|  | 8×12 | 282 | 0.180 |  |  |  |
| 470 | 8×12 | 391 | 0.140 | 8×16 | 552 | 0.100 |
| 680 | 8×16 | 680 | 0.100 | 8×20 | 780 | 0.090 |
|  |  |  |  | 10×12.5 | 712 | 0.085 |
| 820 | 8×16 | 680 | 0.090 | 8×20 | 780 | 0.080 |
|  | 8×20 | 772 | 0.085 | 8×16 | 791 | 0.064 |
| 1000 | 8×16 | 680 | 0.089 | 10×16 | 892 | 0.068 |
|  | 8×20 | 772 | 0.065 | 8×20 | 870 | 0.065 |
|  | 10×12.5 | 712 | 0.090 | 10×20 | 982 | 0.050 |
| 1200 | 10×16 | 807 | 0.064 | 8×20 | 870 | 0.065 |
|  | 8×16 | 692 | 0.067 | 10×20 | 1062 | 0.044 |
|  |  |  |  | 16×20 | 892 | 0.068 |
| 1500 | 10×20 | 1062 | 0.044 | 10×25 | 1105 | 0.039 |
|  | 10×16 | 956 | 0.055 | 10×20 | 995 | 0.044 |
| 2200 | 10×20 | 1062 | 0.044 | 10×25 | 1155 | 0.039 |
|  | 10×25 | 1080 | 0.041 | 10×30 | 1206 | 0.035 |
|  | 13×20 | 1132 | 0.043 | 13×20 | 1190 | 0.038 |
| 3300 | 10×30 | 1300 | 0.035 | 13×25 | 1462 | 0.030 |
|  | 13×20 | 1245 | 0.038 |  |  |  |
|  | 13×25 | 1370 | 0.035 |  |  |  |
| 4700 | 13×25 | 1732 | 0.030 | 13×36 | 1882 | 0.022 |
|  | 16×25 | 1795 | 0.028 | 13×40 | 2013 | 0.020 |
|  |  |  |  | 16×25 | 1795 | 0.024 |

Max Allowable Ripple Current:/105℃, 100KHzImpedance:/20℃, 100KHz

# STANDARD RATINGS

| Voltage Item Cap.( μF ) | 16V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 47 | 5×11 | 148 | 0.800 |
| 68 | 5×11 | 150 | 0.800 |
| 100 | 6.3×11 | 246 | 0.350 |
| 120 | 6.3×11 | 250 | 0.320 |
| 150 | 6.3×11 | 250 | 0.320 |
| 220 | 8×12 | 391 | 0.140 |
| 330 | 8×12 | 391 | 0.140 |
|  | 8×16 | 552 | 0.100 |
| 470 | 8×16 | 552 | 0.100 |
|  | 8×20 | 690 | 0.090 |
|  | 10×12.5 | 637 | 0.095 |
|  | 10×16 | 791 | 0.064 |
| 680 | 8×20 | 690 | 0.090 |
|  | 10×16 | 791 | 0.064 |
| 820 | 10×20 | 995 | 0.044 |
| 1000 | 10×25 | 1105 | 0.039 |
|  | 10×20 | 995 | 0.044 |
| 1200 | 13×20 | 1190 | 0.038 |
| 1150 | 10×30 | 1513 | 0.035 |
|  | 13×20 | 1411 | 0.036 |
| 2200 | 13×25 | 1657 | 0.030 |
| 3300 | 13×36 | 1882 | 0.022 |
|  | 16×25 | 1795 | 0.024 |

Max Allowable Ripple Current:/105℃, 100KHz Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 25V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 10 | 5×11 | 62 | 5.200 |
| 15 | 5×11 | 86 | 3.600 |
| 22 | 5×11 | 100 | 2.400 |
| 33 | 5×11 | 120 | 1.200 |
| 47 | 5×11 | 161 | 0.800 |
| 68 | 6.3×12 | 200 | 0.370 |
| 100 | 6.3×12 | 255 | 0.350 |
| 120 | 8×12 | 300 | 0.200 |
| 150 | 8×12 | 550 | 0.140 |
| 220 | 8×16 | 552 | 0.100 |
|  | 8×20 | 626 | 0.090 |
| 330 | 8×16 | 552 | 0.085 |
|  | 8×20 | 680 | 0.069 |
|  | 10×12.5 | 630 | 0.090 |
| 470 | 10×16 | 892 | 0.063 |
| 680 | 10×20 | 955 | 0.044 |
| 820 | 10×20 | 955 | 0.044 |
|  | 13×20 | 995 | 0.039 |
| 1000 | 13×20 | 1190 | 0.038 |
| 1200 | 13×25 | 1445 | 0.029 |
| 1500 | 13×30 | 1657 | 0.026 |
|  | 16×25 | 1672 | 0.028 |

Max Allowable Ripple Current:/105℃, 100KHz Impedance:/20℃, 100KHz

# STANDARD RATINGS

| Voltage Item Cap.( μF ) | 35V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 4.7 | 5×11 | 97 | 2.000 |
| 6.8 | 5×11 | 120 | 1.850 |
| 10 | 5×11 | 119 | 1.700 |
| 15 | 5×11 | 150 | 0.900 |
| 22 | 5×11 | 161 | 0.800 |
| 33 | 5×11 | 161 | 0.800 |
| 47 | 6.3×11 | 180 | 0.370 |
| 68 | 6.3×11 | 180 | 0.350 |
| 100 | 8×12 | 391 | 0.180 |
| 120 | 8×12 | 391 | 0.180 |
| 150 | 8×16 | 552 | 0.140 |
| 220 | 10×12.5 | 637 | 0.150 |
|  | 8×20 | 690 | 0.120 |
| 330 | 10×20 | 1062 | 0.072 |
| 470 | 10×25 | 1105 | 0.052 |
|  | 10×20 | 995 | 0.072 |
| 680 | 13×20 | 1190 | 0.050 |
| 820 | 13×20 | 1190 | 0.050 |
| 1000 | 13×25 | 1445 | 0.035 |
| 1200 | 13×30 | 1650 | 0.030 |
|  | 16×25 | 1710 | 0.028 |
| 1500 | 16×25 | 1785 | 0.028 |

Max Allowable Ripple Current:/105℃, 100KHz  Impedance:/20℃, 100KHz

# STANDARD RATINGS

| Voltage Item Cap.( μF ) | 50V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 4.7 | 5×11 | 76 | 2.000 |
| 6.8 | 5×11 | 90 | 1.850 |
| 10 | 5×11 | 93 | 1.700 |
| 15 | 5×11 | 136 | 1.200 |
| 22 | 5×11 | 178 | 0.700 |
| 33 | 6.3×11 | 391 | 0.600 |
| 47 | 6.3×11 | 550 | 0.520 |
| 68 | 8×12 | 650 | 0.350 |
| 100 | 8×16 | 650 | 0.250 |
| 120 | 8×20 | 600 | 0.200 |
| 150 | 8×20 | 520 | 0.180 |
|  | 10×12.5 | 600 | 0.160 |
| 220 | 10×16 | 520 | 0.119 |
| 330 | 10×25 | 807 | 0.072 |
|  | 10×20 | 730 | 0.090 |
| 470 | 13×20 | 935 | 0.060 |
| 680 | 13×25 | 1055 | 0.050 |
| 820 | 16×25 | 1248 | 0.040 |
| 1000 | 16×25 | 1360 | 0.035 |

Max Allowable Ripple Current:/105℃, 100KHz

Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 63V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 12 | 5×11 | 55 | 2.30 |
| 18 | 5×11 | 55 | 2.30 |
| 22 | 6.3×12 | 115 | 1.80 |
| 33 | 6.3×12 | 115 | 1.20 |
| 47 | 8×12 | 232 | 1.00 |
| 68 | 8×12 | 232 | 1.00 |
| 100 | 8×16 | 300 | 0.80 |
| 120 | 10×16 | 357 | 0.60 |
| 150 | 8×20 | 362 | 0.70 |
| 220 | 10×20 | 466 | 0.42 |
|  | 10×25 | 531 | 0.40 |
| 330 | 10×30 | 663 | 0.30 |
|  | 13×20 | 690 | 0.32 |
| 470 | 16×20 | 1040 | 0.18 |
| 680 | 16×25 | 1250 | 0.14 |
| 820 | 16×30 | 1570 | 0.10 |
|  | 18×25 | 1490 | 0.12 |
| 1000 | 16×35 | 1790 | 0.09 |

Max Allowable Ripple Current:/105℃, 100KHz Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 100V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 6.8 | 5×11 | 55 | 2.30 |
| 15 | 6.3×12 | 115 | 2.00 |
| 27 | 8×12 | 232 | 1.20 |
| 39 | 8×16 | 300 | 0.90 |
| 47 | 10×13 | 288 | 0.80 |
| 68 | 10×16 | 357 | 0.60 |
| 100 | 10×25 | 531 | 0.40 |
| 120 | 13×20 | 690 | 0.30 |
| 150 | 16×16 | 795 | 0.25 |
| 220 | 13×30 | 905 | 0.20 |
|  | 16×20 | 1040 | 0.18 |
| 330 | 18×20 | 1240 | 0.15 |
| 470 | 16×35 | 1790 | 0.09 |
| 680 | 16×25 | 1250 | 0.14 |

Max Allowable Ripple Current:/105℃, 100KHz  Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 160V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 10 | 10×13 | 150 | 4.0 |
| 22 | 10×16 | 208 | 3.3 |
| 33 | 10×25 | 366 | 2.0 |
| 47 | 13×20 | 400 | 1.4 |
| 100 | 16×25 | 675 | 0.7 |
| 220 | 18×35 | 1142 | 0.4 |

Max Allowable Ripple Current:/105℃, 100KHz  Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 200V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 10 | 10×16 | 208 | 4.0 |
| 22 | 10×20 | 266 | 3.0 |
| 33 | 13×20 | 366 | 2.0 |
| 47 | 13×25 | 500 | 1.3 |
| 100 | 16×30 | 967 | 0.7 |
| 220 | 18×35 | 1142 | 0.4 |

Max Allowable Ripple Current:/105℃, 100KHz  Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 250V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 3.3 | 8×12 | 108 | 12.0 |
| 4.7 | 10×13 | 138 | 10.0 |
| 10 | 10×20 | 167 | 8.0 |
| 22 | 13×20 | 260 | 3.6 |
| 33 | 13×25 | 300 | 3.2 |
| 47 | 16×25 | 558 | 1.8 |
| 100 | 18×30 | 779 | 0.9 |
| 220 | 18×40 | 833 | 0.8 |

Max Allowable Ripple Current:/105℃, 100KHz  Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 400V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 2.2 | 8×12 | 63 | 6.0 |
| 3.3 | 8×16 | 80 | 5.0 |
| 4.7 | 10×16 | 130 | 4.2 |
| 10 | 13×20 | 300 | 3.5 |
| 22 | 16×25 | 558 | 2.4 |
| 33 | 16×30 | 583 | 1.4 |
| 47 | 18×30 | 717 | 1.0 |

Max Allowable Ripple Current:/105℃, 100KHz   Impedance:/20℃, 100KHz

STANDARD RATINGS

| Voltage Item Cap.( μF ) | 450V |  |  |
| --- | --- | --- | --- |
|  | Case size (mm) | Ripple Current (mA) | Impedance (Ω) |
| 1 | 8×12 | 45 | 21.0 |
| 2.2 | 10×13 | 95 | 18.0 |
| 3.3 | 10×16 | 110 | 12.0 |
| 4.7 | 10×20 | 135 | 7.0 |
| 10 | 13×20 | 180 | 5.0 |
| 22 | 16×25 | 400 | 2.0 |
| 33 | 18×30 | 520 | 1.2 |

Max Allowable Ripple Current:/105℃, 100KHz  Impedance:/20℃, 100KHz